## Slide 1
HACKERFAB DIY-ALD
MODELING CONTEXT
EXECUTION RUNTIMES
Real-world hardware runtime: 13,920.0 seconds (232 min / ~4 hrs)
INPUT PARAMETERS
OUTPUT FILES
Chronological step-by-step state logging file (.log / .txt)
Requires physical Arduino hardware to control system valves
Unfeasible for software-only process simulation
Tested using a custom Python script to emulate the physical valve-switching sequence
Purge time: 3,000 ms
Precursor pulse counts: 8, 12, 4
Precursor pulse times: 500 ms, 200 ms, 1,200 ms
Heater temperatures (4 zones): 300°C, 180°C, 120°C, 250°C
•
•
•
•
•
•
•

## Slide 2
DREAM-ALD
MODELING METHOD
MATLAB/Octave-based analytical deposition simulator
INPUT PARAMETERS
EXECUTION RUNTIMES
OUTPUT FILES & DATA
Higher temperature improves film conformality; higher gas pressure increases film penetration depth.
Temperature: 150.0°C and 200.0°C
Precursor pressure: 50.0 Pa and 100.0 Pa
Carrier gas: 50 kPa
Cycle settings: 0.20s pulse, 2.00s purge, 500 total cycles
Channel size: 500 µm width, 10.0 µm height, 1,000 µm length (100 points)
Total run time (Wall-clock): 229.29 seconds (for 500 cycles) = ~ 4 min
Average computation time per cycle: ~458 milliseconds
Thickness profile array (Mean thickness: 0.162 nm)
Film conformality (97.9%) and uniformity (97.5%)
Channel height reduction tracking (Final height: 9.918 µm)
•
•
•
•
•
•
•
•
•
•

## Slide 3
MACHBALL
MODELING METHOD
Python-based Monte Carlo transport simulator
INPUT PARAMETERS
EXECUTION RUNTIMES
OUTPUT FILES & DATA
Wafer shapes: Via (Aspect Ratio = 100, 100 segments) and Trench (Aspect Ratio = 100, 200 segments)
Temperature: 473 K (200°C)
Precursor pressure: 50 Pa and 100 Pa
Sticking probability: 0.01 and 0.02
Total run time (Wall-clock): < 2.0 seconds
Simulation steps: 98 time-steps to reach full saturation
Surface coverage fraction array (0.0 to 1.0 along trench depth)
Conformality (96.54%) and uniformity (95.11%)
Time to reach 90% bottom coverage (t90): 0.082s (at 50 Pa) vs 0.041s (at 100 Pa) (2x speedup)
•
•
•
•
•
•
•
•
•

## Slide 4
NVIDIA PHYSICSNEMO
MODELING METHOD
PyTorch Fourier Neural Operator (FNO) model running on Tesla T4 GPU (15.6 GB)
INPUT PARAMETERS
EXECUTION RUNTIMES
OUTPUT FILES & DATA
GPU-accelerated AI models can replace slow physical simulations with millisecond-level predictions while keeping high accuracy.
Model size: Baseline FNO (5,377 parameters) and Fast FNO (1,137 parameters)
Grid size: 64x64, 128x128, and 256x256 resolutions
Training settings: 20 epochs, 100 training samples
Baseline 256x256 training time: 17.16 seconds total (1.72s per epoch)
Fast 64x64 training time: 0.41 seconds total
Inference time: 1.52 to 2.22 milliseconds per sample (up to 22,864 samples/second)
Trained model weight files (.pt / .pth formats)
Loss progress data (94.1% reduction in training loss)
•
•
•
•
•
•
•
•